White Paper WP120502 Cv Values for Copeland Valves

| Cv Values for Various Bore Sizes |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Valve Sizes |  | ANSI CLASS |  |  |  |  |  |  |
| NPS | DN | 150# | 300# | 600# | 900# | 1,500# | 2500# | 4500# |
| 3/4" | 20 | (0.75) 50 | (0.75)43 | (0.75)43 | (0.68) 24 | (0.68) 24 | (0.56) 13 |  |
| 1" | 25 | (1.00) 88 | (1.00) 78 | (1.00) 68 | (0.81) 35 | (0.81) 35 | (0.56) 12 |  |
| 1" x 3/4" | 25 | 31 | 31 | 31 | 41 | 41 | 29 | 29 |
| 1 1/2" | 40 | (1.50) 225 | (1.50) 210 | (1.50) 190 | (1.34) 125 | (1.34) 125 | (1.10) 84 | 84 |
| 1 1/2" x 1" | 40 | 48 | 48 | 48 | 54 | 54 | 81 | 81 |
| 2" | 50 | (2.00) 498 | (2.00) 470 | (2.00) 450 | (1.68) 432 | (1.68) 432 | (1.50) 140 |  |
| 2 1/2" | 65 | (2.50) 800 | (2.50) 710 | (2.50) 610 | (2.12) 350 | (2.12) 350 | (1.75) 195 |  |
| 3" | 80 | (3.00) 1250 | (3.00) 1200 | (2.90) 1180 | (2.90) 1070 | (2.63) 980 | (2.30) 370 |  |
| 3" x 2" | 80 | 195 | 195 | 195 | 206 | 218 | 333 | 312 |
| 4" | 100 | (4.00) 2500 | (4.00) 2200 | (3.88) 2160 | (3.88) 2000 | (3.44) 1750 | (3.15) 1280 |  |
| 4" x 3" | 100 | 700 | 770 | 520 | 550 | 630 | 1050 | 970 |
| 6" | 150 | (6.00) 5400 | (6.00) 5250 | (5.75) 5100 | (5.75) 4640 | (5.12) 4000 | (4.8) 3200 |  |
| 6" x 3" | 150 | 353 | 353 | 353 | 361 | 377 | 457 | 400 |
| 6"x 4" | 150 | 788 | 788 | 788 | 830 | 917 | 1,516 | 1,100 |
| 8" | 200 | (8.00) 10000 | (8.00)9800 | (7.25) 9300 | (7.25)8100 | (7.00) 7100 | (5.75) 4100 |  |
| 8" x 6" | 200 | 2,500 | 2,101 | 2,162 | 2,376 | 7,815 | 4,641 | 3,050 |
| 10" | 250 | (10.00) 16000 | (10.00) 14850 | (9.75) 14100 | (9.38) 12000 | (8.75) 9300 | (7.25) 5000 |  |
| 10" x 8" | 250 | 4,500 | 4,250 | 4,500 | 5,000 | 6,250 | 7,600 | 7,020 |
| 12" | 300 | (12.00) 24000 | (12.00) 22000 | (11.75) 20800 | (11.12) 18600 | (10.38) 16000 | (8.82) 7400 |  |
| 12" x 8" | 300 | 3,200 | 3,200 | 3,300 | 3,500 | 4,000 | 6,600 | 4,150 |
| 12" x 10" | 300 | 7,349 | 7,349 | 7,778 | 9,270 | 12,400 | 10,900 | 14,000 |

Notes:

- Actual bore sizes for full bore ball valves are given in parenthesis.

- Weld-in valve prices may be significantly affected through the careful selection of bore sizes.

| Cv Values for Various Bore Sizes (continued) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 14" | 350 | ( 13.12) 31000 | (13.12) 29000 | ( 12.25) 24000 | (12.25) 21800 | (11.25) 18800 |  |  |
| 14" x 10" | 350 | 5,950 | 5,950 | 6,300 | 7,000 | 8,600 | 13400 | 9100 |
| 14" x 12" | 350 | 13,794 | 13,794 | 15,502 | 19,582 | 19,466 | 13347 | 18800 |
| 16" | 400 | (15.00) 43000 | (15.00) 41000 | (14.00)31000 | (14.00) 28000 | (12.81) 25000 |  |  |
| 16" x 12" | 400 | 9,301 | 9,301 | 10,013 | 11,487 | 14,864 |  |  |
| 16" x 14" | 400 | 19,917 | 19,917 | 23,041 | 30,124 | 25,787 |  |  |
| 18" | 450 | (16.88) 57000 | ( 16.88) 54000 | (15.75) 39000 | (15.75) 36000 | 32000 |  |  |
| 18" x 12" | 450 | 7,571 | 7,725 | 8,074 | 8,735 | 10228 |  |  |
| 18" x 14" | 450 | 13,591 | 14,080 | 15,242 | 17,642 | 24039 |  |  |
| 20" | 500 | (18.81) 56000 | (18.81) 53000 | (17.5) 50000 | (17.5) 45000 | 40000 |  |  |
| 20" x 14" | 450 | 11,010 | 11,242 | 12,068 | 13,151 | 15594 |  |  |
| 20" x 16" | 450 | 18,879 | 19,553 | 22,079 | 25,726 | 35175 |  |  |
| 24" | 600 | (22.62) 75000 | (22.62) 73000 | (21.00) 70000 | (19.5) 67000 | 59000 |  |  |
| 24" x 20" | 600 | 32,666 | 33,793 | 39,620 | 48,754 | 70991 |  |  |
| 30" | 750 | 82,350 | 79,000 | 74,500 | 71,600 | 62800 |  |  |
| 32" | 800 | 155,000 | 152,000 | 134,000 | 123,000 | 108000 |  |  |
| 36" | 900 | 199,000 | 185,000 | 182,500 | 167,000 | 147000 |  |  |

|  | Ferralium® alloy 255 (UNS S32550) Fe 62, Cr 25.5, Ni 5.5, Mo 3.4 Cu 2.0, Mn 1.6, Si 0.7, N 0.2 Mining, Industrial and Marine Applications for Alloy 255 ## Topics Covered. Background Characterisation of Stainless Steels Martensitic Alloys Semi-austenitic Alloys Austenitic Alloys Properties of Stainless Steels Strength of Stainless Steels Heat Treatmet Typical Chemical Composition of Stainless Steels Typical Mechanical Properties of Stainless Steels Typical Physical Properties of Stainless Steels Alloy Designations Corrosion Resistance of Stainless Steels Heat Resistance of Stainless Steels Fabrication of Stainless Steels Cold Working of Stainless Steels Hot Working of Stainless Steels Machinability Welding of Stainless Steels Applications of Stainless Steels Supplied Forms. ## Background. Precipitation hardening stainless steels are chromium and nickel containing steels that provide an optimum combination of the properties of martensitic and austenitic grades. Like martensitic grades, they are known for their ability to gain high strength through heat treatment and they also have the corrosion resistance of austenitic stainless steels. The high tensile strengths of precipitation hardening stainless steels come after a heat treatment process that leads to precipitation hardening of a martensitic or austenitic matrix. Hardening is achieved through the addition of one or more of the elements Copper, Aluminium, Titanium, Niobium, and Molybdenum. The most well known precipitation hardening steel is 17-4 PH. The name comes from the additions 17% Chromium and 4% Nickel. It also contains 4% Copper and 0.3% Niobium. 17-4 PH is also known as stainless steels grade 630. The advantage of precipitation hardening steels is that they can be supplied in a “solution treated” condition, which is readily machineable. After machining or another fabrication method, a single, low temperature heat treatment can be applied to increase the strength of the steel. This is known as ageing or age-hardening. As it is carried out at low temperature, the component undergoes no distortion.. ## Characterisation of Stainless Steels Precipitation hardening stainless steels are characterised into one of three groups based on their final microstructures after heat treatment. The three types are: martensitic (e.g. 17-4 PH), semi-austenitic (e.g. 17-7 PH) and austenitic (e.g. A-286). ## Martensitic Alloys Martensitic precipitation hardening stainless steels have a predominantly austenitic structure at annealing temperatures of around 1040 to 1065°C. Upon cooling to room temperature, they undergo a transformation that changes the austenite to martensite. ## Semi-austenitic Alloys Unlike martensitic precipitation hardening steels, annealed semi-austenitic precipitation hardening steels are soft enough to be cold worked. Semi-austenitc steels retain their austenitic structure at room temperature but will form martensite at very low temperatures. ## Austenitic Alloys Austenitic precipitation hardening steels retain their austenitic structure after annealing and hardening by ageing. At the annealing temperature of 1095 to 1120°C the precipitation hardening phase is soluble. It remains in solution during rapid cooling. When reheated to 650 to 760°C, precipitation occurs. This increases the hardness and strength of the material. Hardness remains lower than that for martensitic or semi-austenitic precipitation hardening steels ustenitic alloys remain nonmagnetic. ## Properties of Stainless Steels ## Strength of Stainless Steels Yield strengths for precipitation-hardening stainless steels are 515 to 1415 MPa. Tensile strengths range from 860 to 1520 MPa. Elongations are 1 to 25%. Cold working before ageing can be used to facilitate even higher strengths. ## Heat Treatment of Stainless Steels The key to the properties of precipitation hardening stainless steels lies in heat treatment. After solution treatment or annealing of precipitation hardening stainless steels, a single low temperature “age hardening” stage is employed to achieve the required properties. As this treatment is carried out at a low temperature, no distortion occurs and there is only superficial discolouration. During the hardening process a slight decrease in size takes place. This shrinking is approximately 0.05% for condition H900 and 0.10% for H1150. Typical mechanical properties achieved for 17-4 PH after solution treating and age hardening are given in the following table. Condition designations are given by the age hardening temperature in °F. Table 1. Mechanical property ranges after solution treating and age hardening Cond.; Hardening Temp and time; Hardness (Rockwell C); Tensile Strength (MPa). A; Annealed; 36; 1100. H900; 482°C, 1 hour; 44; 1310. H925; 496°C, 4 hours; 42; 1170-1320. H1025; 552°C, 4 hours; 38; 1070-1220. H1075; 580°C, 4 hours; 36; 1000-1150. H1100; 593°C, 4 hours; 35; 970-1120. H1150; 621°C, 4 hours; 33; 930-1080.. ## Typical Chemical Composition of Stainless Steels Table 2. Typical chemical composition for stainless steelsalloy 17-4PH 17-4 PH. C; 0.0-0.07. Mn; 0.0-1.5. Si; 0.0-0.7. P; 0.0-0.04. S; 0.0-0.02. Cr; 15.0-17.0. Ni; 3.0-5.0. Cu; 3.0-5.0. Nb; 0.0-0.45. Mo; 0.0-0.6. Fe; Balance. ## Typical Mechanical Properties of Stainless Steels Table 3. Typical mechanical properties for stainless steels alloy 17-4PH Grade 17-4PH; Annealed; Cond 900; Cond 1150. Tensile Strength (MPa); 1100; 1310; 930. Elongation A5 (%); 15; 10; 16. Proof Stress 0.2% (MPa); 1000; 1170; 724. Elongation A5 (%); 15; 10; 16. ## Typical Physical Properties of Stainless Steels Table 4. Typical physical properties for stainless steels alloy 17-4PH Property; Value. Density; 7.75 kg/m3. Modulus of Elasticity; 196 GPa. Electrical Resistivity; 0.080x10-6Ω.m. Thermal Conductivity; 18.4 W/m.K. Thermal Expansion; 10.8x10-6 /K. ## Alloy Designations Stainless steels 17-4 PH also corresponds to a number of following standard designations and specifications. Table 5. Alternate designations for stainless steels alloy 17-4PH Euronorm; UNS; BS; En; Grade. 1.4542; S17400; -; -; 630.. ## Corrosion Resistance of Stainless Steels Precipitation hardening stainless steels have moderate to good corrosion resistance in a range of environments. They have a better combination of strength and corrosion resistance than when compared with the heat treatable 400 series martensitic alloys. Corrosion resistance is similar to that found in grade 304 stainless steels. In warm chloride environments, 17-4 PH is susceptible to pitting and crevice corrosion. When aged at 550°C or higher, 17-4 PH is highly resistant to stress corrosion cracking. Better stress corrosion cracking resistance comes with higher ageing temperatures. Corrosion resistance is low in the solution treated (annealed) condition and it should not be used before heat treatment. ## Heat Resistance of Stainless Steels 17-4 PH has good oxidation resistance. In order to avoid reduction in mechanical properties, it should not be used over its precipitation hardening temperature. Prolonged exposure to 370-480°C should be avoided if ambient temperature toughness is critical. ## Fabrication of Stainless Steels Fabrication of all stainless steels should be done only with tools dedicated to stainless steel materials or tooling and work surfaces must be thoroughly cleaned before use. These precautions are necessary to avoid cross contamination of stainless steels by easily corroded metals that may discolour the surface of the fabricated product. ## Cold Working of Stainless Steels Cold forming such as rolling, bending and hydroforming can be performed on 17-4PH but only in the fully annealed condition. After cold working, stress corrosion resistance is improved by re-ageing at the precipitation hardening temperature. ## Hot Working of Stainless Steels Hot working of 17-4 PH should be performed at 950°-1200°C. After hot working, full heat treatment is required. This involves annealing and cooling to room temperature or lower. Then the component needs to be precipitation hardened to achieve the required mechanical properties. ## Machinability In the annealed condition, 17-4 PH has good machinability, similar to that of 304 stainless steels. After hardening heat treatment, machining is difficult but possible. Carbide or high speed steel tools are normally used with standard lubrication. When strict tolerance limits are required, the dimensional changes due to heat treatment must be taken into account ## Welding of Stainless Steels Precipitation hardening steels can be readily welded using procedures similar to those used for the 300 series of stainless steels. Grade 17-4 PH can be successfully welded without preheating. Heat treating after welding can be used to give the weld metal the same properties as for the parent metal. The recommended grade of filler rods for welding 17-4 PH is 17-7 PH.. ## Applications of Stainless Steels Due to the high strength of precipitation hardening stainless steels, most applications are in aerospace and other high-technology industries. Applications include:  Gears  Valves and other engine components  High strength shafts  Turbine blades  Moulding dies  Nuclear waste casks. |  |  |  |
| --- | --- | --- | --- | --- |