White Paper WP120808 Valve Body Material Selections

This paper is to help address some of the common issues surrounding the specification of valve body materials and body dimensions. It is not all-conclusive but is meant to provide a general introduction. In general, most valve manufacturers depend upon the customer to provide specifications regarding the valve body material. The valve body is typically the same material as the surrounding pipe. Bodies made of forgings are typically viewed as superior to cast bodies which may contain porosity and have less strength.

| COMMON ABBREVIATIONS IN THE VALVE INDUSTRY |  |  |  |
| --- | --- | --- | --- |
| ANSI | American National Standards Institute | API | American Petroleum Institute |
| ASME | American Society of Mechanical Engineers | ASTM | American Society for Testing Materials |
| BS | British Standards | DIN | Deutsche Industrie - Normen |
| BVQI | Bureau Veritas Quality International | ISO | International Standards Organisation |
| VALVE MATERIALS |  |  |  |
| Br | Bronze | A.I. | All Iron |
| C.I. | Cast Iron | M.I. | Malleable Iron |
| N.I. | Nickel Iron | D.I. | Ductile Iron |
| C.S. | Cast Steel/Carbon Steel | F.S. | Forged Steel |
| S.S. | Stainless Steel | PVC | Polyvinyl Chloride |
| N | Nickel | M | Monel Metal |
| Mo | Molybdenum | Al | Aluminium |
| Cr | Chromium | Tef | Teflon |
| 13% Cr | Type 410 Stainless Steel | HF | Hard Face (Stellite Face) |
| OPERATING MECHANISMS |  |  |  |
| O.S. & Y | Outside Screw & Yoke | N.R.S. | Non Rising Stem |
| R.S. | Rising Stem | . | . |
| END CONNECTIONS |  |  |  |
| F.E. | Flanged Ends | S.E. | Screwed Ends |
| F.F.D. | Flanged, Faced & Drilled | B.W. | Butt Welding Ends |
| S.W. | Socket Welding Ends | Scr. | Screwed Ends |
| Flg. | Flanged Ends | RTJ | Ring Type Joint |

| VALVE MATERIAL TEMPERATURE LIMITS |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DEGREES F |  |  |  |  |  |  |  |
| VALVE BODY MATERIAL |  |  |  |  |  |  |  |
| MATERIAL |  |  | LOWER |  | UPPER |  |  |
| Cast Iron |  |  | -20 |  | 410 |  |  |
| Ductile Iron |  |  | -20 |  | 650 |  |  |
| Carbon Steel - Grade WCB |  |  | -20 |  | 1000 |  |  |
| Carbon Steel - Grade LCB |  |  | -50 |  | 650 |  |  |
| Carbon Moly - Grade WC1 |  |  | -20 |  | 850 |  |  |
| 1 1/4 Cr - 1/2 Mo - Grade WC6 |  |  | -20 |  | 1000 |  |  |
| 2 1/4 Cr - 1 Mo - Grade WC9 |  |  | -20 |  | 1050 |  |  |
| 5 Cr - 1/2 Mo - Grade C5 |  |  | -20 |  | 1100 |  |  |
| 9 Cr. - 1 Mo - Grade C12 |  |  | -20 |  | 1100 |  |  |
| Type 304 SS - Grade CF8 |  |  | -425 |  | 1500 |  |  |
| Type 347 SS - Grade CF8C |  |  | -425 |  | 1500 |  |  |
| Type 316 SS - Grade CF8M |  |  | -425 |  | 1500 |  |  |
| 3 1/2 Ni - Grade LC3 |  |  | -150 |  | 650 |  |  |
| Aluminium |  |  | -325 |  | 400 |  |  |
| Bronze |  |  | -325 |  | 550 |  |  |
| Inconel |  |  | -325 |  | 1200 |  |  |
| Monel |  |  | -325 |  | 900 |  |  |
| Hastelloy B |  |  | -325 |  | 700 |  |  |
| Hastelloy C |  |  | -325 |  | 1000 |  |  |
| Titanium |  |  | . |  | 600 |  |  |
| Nickel |  |  | -325 |  | 500 |  |  |
| Alloy 20 |  |  | -50 |  | 300 |  |  |
| VALVE TRIM MATERIAL |  |  |  |  |  |  |  |
| Type 304 SS |  |  | 450 |  | 600 |  |  |
| Type 316 SS |  |  | 450 |  | 600 |  |  |
| Hastelloy B |  |  | . |  | 700 |  |  |
| Hastelloy C |  |  | . |  | 1000 |  |  |
| Alloy 20 |  |  | -50 |  | 600 |  |  |
| Type 416 410 SS 40 RC |  |  | -20 |  | 800 |  |  |
| TFE |  |  | -450 |  | 450 |  |  |
| MATERIAL COMPARISON FOR CAST AND FORGED PRODUCTS |  |  |  |  |  |  |  |
| GENERAL CLASSIFICATION | CASTINGS |  |  | FORGINGS |  |  |  |
|  | ASTM | BS |  | ASTM |  | BS |  |
| Carbon Steel | A216 - WCA | - |  | A105 |  | 1503 - 161B |  |
|  | - | 1504 - 161 |  | - |  | - |  |
|  | A216 - WCB | 1504 - B |  | A105 |  | 1503 - 161C |  |
|  | A216 - WCC | - |  | - |  | - |  |
|  | - | 1504 - C |  | - |  | - |  |
| Carbon - 1/2 Mo | A217 - WC1 | 1504 - 240 |  | A182 - F1 |  | 1503 - 240B |  |
| 1/2 Cr - 1/2 Mo - 1/2 Ni | - WC4 | - |  | - |  | - |  |
| 1 Cr - 1/2 Mo - 1/2 Ni | A217 - WC5 | - |  | A182 - F12 |  | 1503 - 620 |  |
| 1 1/4 Cr - 1/2 Mo | - WC6 | 1504 - 621 |  | - F11 |  | - |  |
| 2 1/4 Cr - 1 Mo | - WC9 | - 622 |  | - F22 |  | 1503 - 622 |  |
| 3 Cr - 1 Mo | . | . |  | - F21 |  | . |  |
| 5 Cr - 1/2 Mo (C0.15) | . | . |  | - F5 |  | . |  |
| 5 Cr - 1/2 Mo (C0.25) | A217 - C5 | 1504 - 625 |  | - F5a |  | 1503 - 625 |  |
| 9 Cr - 1 Mo | A217 - C12 | - 629 |  | - F9 |  | . |  |
| Carbon Steel for Low Temp. | A352 - LCB | 4242 - GRA |  | A350 - LF1 |  | . |  |
| 13 Cr | A217 - CA15 | . |  | A182 - F6 |  | 1503 - 713 |  |
| 18 Cr - 8 Ni (C0.03) | A351 - CF3 | . |  | - F304L |  | . |  |
| 18 Cr - 8 Ni (C0.08) | - CF8 | . |  | - F304 |  | - 801 |  |
| 18 Cr - 8 Ni - 2 Mo (C0.03) | A351 - CF3M | . |  | - F316L |  | . |  |
| 18 Cr - 8 Ni - 2 Mo (C0.08) | - CF8M | 1632 - GRC |  | - F316 |  | - 8453 |  |
| 18 Cr - 8 Ni - Cb (C0.08) | A351 - CF8C | . |  | - F347 |  | - 821Nb |  |
| 22 Cr - 12 Ni (C0.08) | - CH18 | . |  | . |  | . |  |
| 8 Cr - 20 Ni (C0.20) | . | . |  | A182 - F10 |  | . |  |
| HASTELLOY.B | A494 - N - 12MV | . |  | . |  | . |  |

PRESSURE - TEMPERATURE RATINGS
ASME B16.34 - 1996 - STANDARD CLASS

| ASTM A216 Gr. WCB (A105) TEMP °F; WORKING PRESSURE (in psig) BY CLASS. 150; 300; 600; 900; 1500; 2500. -20 to 100 200 300; 285 260 230; 740 675 655; 1480 1350 1315; 2220 2025 1970; 3705 3375 3280; 6170 5625 5470. 400 500 600; 200 170 140; 635 600 550; 1270 1200 1095; 1900 1795 1640; 3170 2995 2735; 5280 4990 4560. 650 700 750; 125 110 95; 535 535 505; 1075 1065 1010; 1610 1600 1510; 2685 2665 2520; 4475 4440 4200. 800 850 900; 80 65 50; 410 270 170; 825 535 345; 1235 805 515; 2060 1340 860; 3430 2230 1430. 950 1000; 35 20; 105 50; 205 105; 310 155; 515 260; 860 430. Not recommended for prolonged use above 800°F | TEMP °C; WORKING PRESSURE (in bar) BY RATING. PN 20; PN 50; PN 100; PN 150; PN 250; PN 420. 38 93 149; 19.7 17.9 15.9; 51.0 46.6 45.2; 102.1 93.1 90.7; 153.1 139.7 135.9; 255.5 232.8 226.2; 425.5 387.9 377.2. 204 260 316; 13.8 11.7 9.7; 43.8 41.4 37.9; 87.6 82.8 75.5; 131.0 123.8 113.1; 218.6 206.6 188.6; 363.4 344.1 314.5. 343 371 399; 8.6 7.6 6.6; 36.9 36.9 34.8; 74.1 73.4 69.7; 111.0 110.3 104.1; 185.2 183.8 173.8; 308.6 306.2 289.7. 427 454 482; 5.5 4.5 3.4; 28.3 18.6 11.7; 56.9 36.9 23.8; 85.2 55.5 35.5; 142.1 92.4 59.3; 236.6 153.8 98.6. 510 538; 2.4 1.4; 7.2 3.4; 14.1 7.2; 21.4 10.7; 35.5 17.9; 59.3 29.7. . |
| --- | --- |

| ASTM A217 Gr WC6 (F11) TEMP °F; WORKING PRESSURE (in psig) BY CLASS. 150; 300; 600; 900; 1500; 2500. -20 to 100 200 300; 290 260 230; 750 750 720; 1500 1500 1445; 2250 2250 2165; 3750 3750 3610; 6250 6250 6015. 400 500 600; 200 170 140; 695 665 605; 1385 1330 1210; 2080 1995 1815; 3465 3325 3025; 5775 5540 5040. 650 700 750; 125 110 95; 590 570 530; 1175 1135 1065; 1765 1705 1595; 2940 2840 2660; 4905 4730 4430. 800 850 900; 80 65 50; 510 485 450; 1015 975 900; 1525 1460 1350; 2540 2435 2245; 4230 4060 3745. 950 1000 1050; 35 20 20(1); 320 215 145; 640 430 290; 955 650 430; 1595 1080 720; 2655 1800 1200. 1100 1150 1200; 20(l) 20(l) 15(l); 95 60 40; 190 125 75; 290 185 115; 480 310 190; 800 515 315. (l) : For weld end valves only. | TEMP °C; WORKING PRESSURE (in bar) BY RATING. PN 20; PN 50; PN 100; PN 150; PN 250; PN 420. 38 93 149; 20.0 17.9 15.9; 51.7 51.7 49.7; 103..4 103.4 9.7; 155.1 155.2 149.3; 258.6 258.6 249.0; 431.0 431.0 414.8. 204 260 316; 13.8 11.7 9.7; 47.9 45.9 41.7; 95.5 91.7 83.4; 143.4 137.6 125.2; 239.0 229.3 208.6; 398.3 382.1 347.6. 343 371 399; 8.6 7.6 6.6; 40.7 39.3 36.6; 81.0 78.3 73.4; 121.7 117.6 110.0; 202.8 195.9 183.4; 338.3 326.2 305.5. 427 454 482; 5.5 4.5 3.4; 35.2 33.4 31.0; 70.0 67.2 62.1; 105.2 100.7 93.1; 175.2 167.9 154.8; 291.7 280.0 258.3. 510 538 566; 2.4 1.4 1.4(l); 22.1 14.8 10.0; 44.1 29.7 20.0; 65.9 44.8 29.7; 110.0 74.5 49.7; 183.1 124.1 82.8. 593 621 649; 1.4(l) 1.4(l) 1.0(l); 6.6 4.1 2.8; 13.1 8.6 5.2; 20.0 12.8 7.9; 33.1 21.4 13.1; 55.2 35.5 21.7. Not to be used over 1100°F(593°C) for flanged ends. |
| --- | --- |

| ASTM A217 Gr. WC9 (F22) TEMP °F; WORKING PRESSURE (in psig) BY CLASS. 150; 300; 600; 900; 1500; 2500. -20 to 100 200 300; 290 260 230; 750 750 730; 1500 1500 1455; 2250 2250 2185; 3750 3750 3640; 6250 6250 6070. 400 500 600; 200 170 140; 705 665 605; 1410 13300 1210; 2115 1995 1815; 3530 3325 3025; 5880 5540 5040. 650 700 750; 125 110 95; 590 570 530; 1175 1135 1065; 1765 1705 1595; 2940 2840 2660; 4905 4730 4430. 950 1000 1050; 80 65 50; 510 485 450; 1015 975 900; 1525 1460 1350; 2450 2435 2245; 4230 4060 3745. 800 850 900; 35 20 20(l); 375 260 175; 755 520 350; 1130 780 525; 1885 1305 875; 3145 2170 1455. 1100 1150 1200; 20(l) 20(l) 20(l); 110 -- --; 220 -- --; 330 -- --; 550 -- --; 915 -- --. (l) : For weld end valves only. | TEMP °C; WORKING PRESSURE (in bar) BY RATING. PN 20; PN 50; PN 100; PN 150; PN 250; PN 420. 38 93 149; 20.0 17.9 15.9; 51.7 51.7 50.3; 103..4 103.4 100.3; 155.2 1552 150.7; 258.6 258.6 251.0; 431.0 431.0 418.6. 204 260 316; 13.8 11.7 9.7; 48.6 45.9 41.7; 97.2 91.7 83.4; 145.9 137.6 125.2; 243.4 229.3 208.6; 405.5 382.1 347.6. 343 371 399; 8.6 7.6 6.6; 40.7 39.3 36.6; 81.0 78.3 73.4; 121.7 117.6 110.0; 202.8 195.9 183.4; 338.3 326.2 305.5. 427 454 482; 5.5 4.5 3.4; 35.2 33.4 31.0; 70.0 67.2 62.1; 105.2 100.7 93.1; 175.2 167.9 154.8; 291.7 280.0 258.3. 510 538 566; 2.4 1.4 1.4(l); 25.9 17.9 12.1; 52.1 35.9 24.1; 77.9 53.8 36.2; 130.0 90.0 60.3; 216.9 149.7 100.3. 593 621 649; 1.4(l) 1.4(l) 1.4(l); 7.6 4.8 2.8; 15.2 9.3 5.5; 22.8 14.1 8.6; 37.9 23.8 14.1; 63.1 39.3 23.8. Not to be used over 1100°F(593°C) for flanged ends. |
| --- | --- |

- BUTTWELDING END DETAILS

- ASME B16.25 - 1997

| Welding end detail for joint without backing ring Welding end details intended for use on 0.88 in. (22 mm) and thinner nominal wall thicknesses | Welding end detail for joint with backing ring Welding end details intended for use on nominal wall thicknesses greater than 0.88 in. (22 mm) |
| --- | --- |

NOTE: Internal surface may be re-formed or machined for dimensions B at root face. Contour within the envelope is manufacturer's option unless otherwise specifically ordered.

|  |  | Pipe Schedule No. | Nominal Pipe Size (inch) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 2.1/2 | 3 | 4 | 5 | 6 | 8 | 10 |
| A | inch | ALL | 2.96 | 3.95 | 4.62 | 5.69 | 6.78 | 8.78 | 10.94 |
|  | mm |  | 75 | 91 | 117 | 144 | 172 | 223 | 278 |
| B | inch | 40 | 2.469 | 3.068 | 4026 | 5.047 | 6.065 | 7.981 | 10.020 |
|  | mm |  | 63 | 78 | 102 | 128 | 154 | 203 | 255 |
|  | inch | 60 |  |  |  |  |  | 7.813 | 9.750 |
|  | mm |  |  |  |  |  |  | 198 | 247 |
|  | inch | 80 | 2.323 | 2.900 | 3.826 | 4.813 | 5.761 | 7.625 | 9.562 |
|  | mm |  | 59 | 74 | 97 | 122 | 146 | 194 | 242 |
|  | inch | 100 |  |  |  |  |  | 7.437 | 9.312 |
|  | mm |  |  |  |  |  |  | 189 | 237 |
|  | inch | 120 |  |  | 3.624 | 4.563 | 5.501 | 7.187 | 9.062 |
|  | mm |  |  |  | 92 | 116 | 140 | 183 | 230 |
|  | inch | 100 |  |  |  |  |  | 7.001 | 8.750 |
|  | mm |  |  |  |  |  |  | 178 | 222 |
|  | inch | 160 | 2.125 | 2.624 | 3.438 | 4.313 | 5.187 | 6.813 | 8.500 |
|  | mm |  | 54 | 67 | 87 | 110 | 132 | 173 | 216 |
|  | inch | XXS | 1.771 | 2.300 | 3.152 | 4.063 | 4.897 | 6.875 |  |
|  | mm |  | 45 | 58 | 80 | 103 | 124 | 175 |  |

|  |  | Pipe Schedule No. | Nominal Pipe Size (inch) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 12 | 14 | 16 | 18 | 20 | 24 |  |
| A | inch | ALL | 12.97 | 14.25 | 16.25 | 18.28 | 20.31 | 24.38 |  |
|  | mm |  | 329 | 362 | 413 | 464 | 516 | 619 |  |
| B | inch | STD | 12.000 | 13.250 | 15.250 | 17.250 | 19.250 | 23.250 |  |
|  | mm |  | 305 | 337 | 387 | 438 | 489 | 591 |  |
|  | inch | XS | 11.750 | 13.000 |  | 17.000 | 19.000 | 23.000 |  |
|  | mm |  | 298 | 330 |  | 432 | 483 | 584 |  |
|  | inch | 30 |  |  |  |  |  | 22.876 |  |
|  | mm |  |  |  |  |  |  | 581 |  |
|  | inch | 40 | 11.938 | 13.124 | 15.000 | 16.876 | 18.812 | 22.624 |  |
|  | mm |  | 303 | 333 | 381 | 429 | 478 | 575 |  |
|  | inch | 60 | 11.626 | 12.812 | 14.688 | 16.500 | 18.376 | 22.062 |  |
|  | mm |  | 295 | 325 | 373 | 419 | 467 | 560 |  |
|  | inch | 80 | 11.374 | 12.500 | 14.312 | 16.124 | 17.938 | 21.562 |  |
|  | mm |  | 289 | 318 | 364 | 410 | 456 | 584 |  |
|  | inch | 100 | 11.062 | 12.124 | 13.938 | 15.688 | 17.438 | 20.938 |  |
|  | mm |  | 281 | 308 | 354 | 398 | 443 | 532 |  |
|  | inch | 120 | 10.750 | 11.812 | 13.562 | 15.250 | 17.000 | 20.376 |  |
|  | mm |  | 273 | 300 | 344 | 387 | 432 | 518 |  |
|  | inch | 140 | 10.500 | 11.500 | 13.124 | 14.876 | 16.500 | 19.876 |  |
|  | mm |  | 267 | 292 | 333 | 378 | 419 | 505 |  |
|  | inch | 160 | 10.126 | 11.188 | 12.812 | 14.438 | 16.062 | 19.312 |  |
|  | mm |  | 257 | 284 | 325 | 367 | 408 | 491 |  |

- MATERIAL COMPOSITION FOR CAST MATERIAL

|  | CARBON STEEL |  |  | ALLOY STEEL |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| ASTM Designation & Grade Identifcation | A216 WCB | A352 LCB | A252 LCC | A217 WC6 | A217 WC9 | A217 CA15 |
| Elements % by weight |  |  |  |  |  |  |
| Carbon | 0.30 $ | 0.30 $ | 0.25 | 0.05-0.20 | 0.05-0.18 | 0.15 |
| Manganese | 1.00 | 1.00 | 1.20 | 0.50 - 0.80 | 0.40 - 0.70 | 1.00 |
| Phosphorus | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.040 |
| Sulphur | 0.045 | 0.045 | 0.045 | 0.045 | 0.045 | 0.040 |
| Silicon | 0.60 | 0.60 | 0.60 | 0.60 | 0.60 | 1.50 |
| Copper | 0.30 * | 0.30 * | 0.30 * | 0.50 * | 0.50 * |  |
| Nickel | 0.50 * | 0.50 * | 0.50 * | 0.50 * | 0.50 * | 1.00 |
| Chromium | 0.50 * | 0.50 * | 0.50 * | 1.00 - 1.50 | 2.00 - 2.75 | 11.5 - 14.0 |
| Molybdenum | 0.20 * | 0.20 * | 0.20 * | 0.45 - 0.65 | 0.90 - 1.20 | 0.50 |
| Vanadium | 0.03 * | 0.03 * | 0.03 * |  |  |  |
| Tungsten |  |  |  | 0.10 * | 0.10 * |  |

* These are residual elements, total content of these shall not exceed 1%.
Values indicated are maximum except when range is given.

| Material | ASTM A194 Gr. B7 | ASTM A320 Gr. L7 | ASTM A194 Gr. 2H | ASTM A194 Gr. 7 | Hardfacing Stellite 6 | ASTM A182 Gr. F6A | ASTM A276 Type 316 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Elements |  |  |  |  |  |  |  |
| Carbon | 0.37 - 0.49 | 0.38 - 0.48 | 0.40 min | 0.37 - 0.49 | 0.90 - 1.40 | 0.150 | 0.80 |
| Manganese | 0.65 - 1.10 | 0.75 - 1.00 | 1.00 | 0.65 - 1.10 | 1.00 | 1.000 | 2.000 |
| Phosphorus | 0.350 | 0.035 | 0.040 | 0.040 |  | 0.040 | 0.045 |
| Sulphur | 0.040 | 0.040 | 0.050 | 0.040 |  | 0.030 | 0.030 |
| Silicon | 0.15 - 0.35 | 0.15 - 0.35 | 0.40 | 0.15 - 0.35 | 2.00 | 1.000 | 1.000 |
| Chromium | 0.75 - 1.20 | 0.80 - 1.10 |  | 0.75 - 1.20 | 26.0 - 32.0 | 11.5 - 13.5 | 16.0 - 18.0 |
| Molybdenum | 0.15 - 0.25 | 0.15 - 0.25 |  | 0.15 - 0.25 | 1.00 |  | 2.0 - 3.0 |
| Nickel |  |  |  |  | 3.00 | 0.50 | 10.0 - 14.0 |
| Cobalt |  |  |  |  | balance |  |  |
| Tungsten |  |  |  |  | 3.0 - 6.0 |  |  |
| Iron |  |  |  |  | 3.00 |  |  |
| Nitrogen |  |  |  |  |  |  |  |

- PIPE FLANGE DIMENSIONS

- ASME B16.5 - 1996

- CLASS 150 STEEL PIPE FLANGE DIMENSIONS :
RAISED FACE

| Nominal size |  | A ø |  | B ø |  | C ø |  | D |  | E ø |  | Bolt |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | in | mm | in | mm | in | mm | in | mm | Number | Dia |
| 2 | 50 | 6.00 | 152 | 4.76 | 120 | 3.62 | 92 | 0.75 (0.62) | 19.1 (15.9) | 0.75 | 19 | 4 | 5/8 |
| 2.1/2 | 65 | 7.00 | 178 | 5.50 | 139 | 4.12 | 105 | 0.88 (0.69) | 22.3 (17.5) | 0.75 | 19 | 4 | 5/8 |
| 3 | 80 | 7.50 | 190 | 6.00 | 152 | 5.00 | 127 | 0.94 (0.75) | 23.9 (19.1) | 0.75 | 19 | 4 | 5/8 |
| 4 | 100 | 9.00 | 229 | 7.50 | 190 | 6.19 | 157 | 0.94 | 23.9 | 0.75 | 19 | 8 | 5/8 |
| 5 | 125 | 10.00 | 254 | 8.50 | 216 | 7.31 | 186 | 0.94 | 23.9 | 0.88 | 22 | 8 | 3/4 |
| 6 | 150 | 11.00 | 279 | 9.50 | 241 | 8.50 | 216 | 1.00 | 25.4 | 0.88 | 22 | 8 | 3/4 |
| 8 | 200 | 13.50 | 343 | 11.75 | 298 | 10.62 | 270 | 1.12 | 28.6 | 0.88 | 22 | 8 | 3/4 |
| 10 | 250 | 16.00 | 406 | 14.25 | 362 | 12.75 | 324 | 1.19 | 30.2 | 1.00 | 25 | 12 | 7/8 |
| 12 | 300 | 19.00 | 483 | 17.00 | 432 | 15.00 | 381 | 1.25 | 31.8 | 1.00 | 25 | 12 | 7/8 |
| 14 | 350 | 21.00 | 533 | 18.75 | 476 | 16.25 | 413 | 1.38 | 35.0 | 1.12 | 29 | 12 | 1 |
| 16 | 400 | 23.50 | 597 | 21.25 | 539 | 18.50 | 470 | 1.44 | 36.6 | 1.12 | 29 | 16 | 1 |
| 18 | 450 | 25.00 | 635 | 22.75 | 578 | 21.00 | 533 | 1.56 | 39.7 | 1.25 | 32 | 16 | 1.1/8 |
| 20 | 500 | 27.50 | 698 | 25.00 | 635 | 23.00 | 584 | 1.69 | 42.9 | 1.25 | 32 | 20 | 1.1/8 |
| 24 | 600 | 32.00 | 813 | 29.50 | 749 | 27.25 | 692 | 1.88 | 47.7 | 1.38 | 35 | 20 | 1.1/4 |

Height of raised face is 0.06" (1.6 mm) each. Dimensions in ( ) are for intergral valve flanges.

- CLASS 300 STEEL PIPE FLANGE DIMENSIONS : RAISED FACE

| Nominal size |  | A ø |  | B ø |  | C ø |  | D |  | E ø |  | Bolt |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | in | mm | in | mm | in | mm | in | mm | Number | Dia |
| 2 | 50 | 6.50 | 165 | 5.00 | 127 | 3.62 | 92 | 0.88 | 22.3 | 0.75 | 19 | 8 | 5/8 |
| 2.1/2 | 65 | 7.50 | 190 | 5.88 | 149 | 4.12 | 105 | 1.00 | 25.4 | 0.88 | 22 | 8 | 3/4 |
| 3 | 80 | 8.25 | 210 | 6.62 | 168 | 5.00 | 127 | 1.12 | 28.6 | 0.88 | 22 | 8 | 3/4 |
| 4 | 100 | 10.00 | 254 | 7.88 | 200 | 6.19 | 157 | 1.25 | 31.8 | 0.88 | 22 | 8 | 3/4 |
| 5 | 125 | 11.00 | 279 | 9.25 | 235 | 7.31 | 186 | 1.38 | 35.0 | 0.88 | 22 | 8 | 3/4 |
| 6 | 150 | 12.50 | 318 | 10.62 | 270 | 8.50 | 216 | 1.44 | 36.6 | 0.88 | 22 | 12 | 3/4 |
| 8 | 200 | 15.00 | 381 | 13.00 | 330 | 10.62 | 270 | 1.62 | 41.3 | 1.00 | 25 | 12 | 7/8 |
| 10 | 250 | 17.50 | 444 | 15.25 | 387 | 12.75 | 324 | 1.88 | 47.7 | 1.12 | 29 | 16 | 1 |
| 12 | 300 | 20.50 | 521 | 17.75 | 451 | 15.00 | 381 | 2.00 | 50.8 | 1.25 | 32 | 16 | 1.1/8 |
| 14 | 350 | 23.00 | 584 | 20.25 | 514 | 16.25 | 413 | 2.12 | 54.0 | 1.25 | 32 | 20 | 1.1/8 |
| 16 | 400 | 25.50 | 648 | 22.50 | 571 | 18.50 | 470 | 2.25 | 57.2 | 1.38 | 35 | 20 | 1.1/4 |
| 18 | 450 | 28.00 | 711 | 24.75 | 628 | 21.00 | 533 | 2.38 | 60.4 | 1.38 | 35 | 24 | 1.1/4 |
| 20 | 500 | 30.50 | 775 | 27.00 | 686 | 23.00 | 584 | 2.50 | 63.5 | 1.38 | 35 | 24 | 1.1/4 |
| 24 | 600 | 36.00 | 914 | 32.00 | 813 | 27.25 | 692 | 2.75 | 69.9 | 1.62 | 41 | 24 | 1.1/2 |

Height of raised face is 0.06" (1.6 mm) each.

- LARGE SIZE PIPE FLANGE DRIILLING DIMENSIONS : AS PER ANSI B16.47 SERIES A

|  | Nominal size |  | A ø |  | B ø |  | C ø |  | D |  | E ø |  | Bolt |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | in | mm | in | mm | in | mm | in | mm | in | mm | in | mm |  |
| Class 150 | 30" | 750 | 38.75 | 984 | 36 | 914 | 33.75 | 857 | 2.94 | 75 | 1.125 | 29 | 28 |
|  | 36" | 900 | 46 | 1168 | 42.75 | 1086 | 40.25 | 1022 | 3.56 | 90 | 1.5 | 38 | 32 |
| Class 300 | 30" | 750 | 43 | 1092 | 39.25 | 997 | 33.75 | 857 | 3.62 | 92 | 1.88 | 48 | 28 |

Height of raised face is 0.06" (1.6mm) each.

- CLASS 600 STEEL PIPE FLANGE DIMENSIONS :
RAISED FACE

| Nominal size |  | A ø |  | B ø |  | C ø |  | D |  | E ø |  | Bolt |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| in | mm | in | mm | in | mm | in | mm | in | mm | in | mm | Number | Dia |
| 2 | 50 | 6.50 | 165 | 5.00 | 127 | 3.62 | 92 | 1.00 | 25.4 | 0.75 | 19 | 8 | 5/8 |
| 2.1/2 | 65 | 7.50 | 190 | 5.88 | 149 | 4.12 | 105 | 1.12 | 28.6 | 0.88 | 22 | 8 | 3/4 |
| 3 | 80 | 8.25 | 210 | 6.62 | 168 | 5.00 | 127 | 1.25 | 31.8 | 0.88 | 22 | 8 | 3/4 |
| 4 | 100 | 10.75 | 273 | 8.50 | 216 | 6.19 | 157 | 1.50 | 38.1 | 1.00 | 25 | 8 | 7/8 |
| 5 | 125 | 13.00 | 330 | 10.50 | 266 | 7.31 | 186 | 1.75 | 44.5 | 1.12 | 29 | 8 | 1 |
| 6 | 150 | 14.00 | 356 | 11.50 | 292 | 8.50 | 216 | 1.88 | 47.7 | 1.12 | 29 | 12 | 1 |
| 8 | 200 | 16.50 | 419 | 13.75 | 349 | 10.62 | 270 | 2.19 | 55.6 | 1.25 | 32 | 12 | 1.1/8 |
| 10 | 250 | 20.00 | 508 | 17.00 | 432 | 12.75 | 324 | 2.50 | 63.5 | 1.38 | 35 | 16 | 1.1/4 |
| 12 | 300 | 22.00 | 559 | 19.25 | 489 | 15.00 | 381 | 2.62 | 66.7 | 1.38 | 35 | 20 | 1.1/4 |
| 14 | 350 | 23.75 | 603 | 20.75 | 527 | 16.25 | 413 | 2.75 | 69.9 | 1.50 | 38 | 20 | 1.3/8 |
| 16 | 400 | 27.00 | 686 | 23.75 | 603 | 18.50 | 470 | 3.00 | 76.2 | 1.62 | 41 | 20 | 1.1/2 |
| 18 | 450 | 29.25 | 743 | 25.75 | 654 | 21.00 | 533 | 3.25 | 82.6 | 1.75 | 45 | 20 | 1.5/8 |
| 20 | 500 | 32.00 | 813 | 28.50 | 724 | 23.00 | 584 | 3.50 | 88.9 | 1.75 | 45 | 24 | 1.5/8 |
| 24 | 600 | 37.00 | 940 | 33.00 | 838 | 27.25 | 692 | 4.00 | 102.0 | 2.00 | 51 | 24 | 1.7/8 |

Height of raised face is 0.25" (6.4 mm) each.

- CLASS 600 PIPE FLANGE DIMENSIONS : RING TYPE

| Valve Size | A ø | B ø | C ø | D | groove number | pitch dia -P | depth E | width F | radius at bottom R |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2 | 6.50 | 5.00 | 4.25 | 1.00 | R23 | 3.250 | 0.312 | 0.469 | 0.03 |
| 2.5 | 7.50 | 5.88 | 5.00 | 1.12 | R26 | 4.000 | 0.312 | 0.469 | 0.03 |
| 3 | 8.25 | 6.62 | 5.75 | 1.25 | R31 | 4.875 | 0.312 | 0.469 | 0.03 |
| 4 | 10.75 | 8.50 | 6.75 | 1.50 | R37 | 5.875 | 0.25 | 0.469 | 0.03 |
| 5 | 13.00 | 10.50 | 8.25 | 1.75 | R41 | 7.125 | 0.312 | 0.469 | 0.03 |
| 6 | 14.00 | 11.50 | 9.50 | 1.88 | R45 | 8.312 | 0.312 | 0.469 | 0.03 |
| 8 | 16.50 | 13.75 | 11.88 | 2.19 | R49 | 10.625 | 0.312 | 0.469 | 0.03 |
| 10 | 20.00 | 17.00 | 14.00 | 2.50 | R53 | 12.750 | 0.312 | 0.469 | 0.03 |
| 12 | 22.00 | 19.25 | 16.25 | 2.62 | R57 | 15.000 | 0.312 | 0.469 | 0.03 |
| 14 | 23.75 | 20.75 | 18.00 | 2.75 | R61 | 16.500 | 0.312 | 0.469 | 0.03 |
| 16 | 27.00 | 23.75 | 20.00 | 3.00 | R65 | 18.500 | 0.312 | 0.469 | 0.03 |
| 18 | 29.25 | 25.75 | 22.62 | 3.25 | R69 | 21.000 | 0.312 | 0.469 | 0.03 |
| 20 | 32.00 | 28.50 | 25.00 | 3.50 | R73 | 23.000 | 0.375 | 0.531 | 0.06 |
| 24 | 37.00 | 33.00 | 29.50 | 4.00 | R77 | 27.250 | 0.438 | 0.656 | 0.06 |

* No. of bolts and bolt dia are same as in C1 600 Raised face.